SECTION 09 72 26

STAINLESS STEEL SHEET WALL COVERING

SECTION 05 58 26

FORMED STAINLESS STEEL TRIM

This Section could also be placed in Division 05 – Metals as Section 05 58 26 –Formed Stainless Steel Trim

This Section includes stainless steel sheet wall covering and associated trim moldings. Products specified in this section may be used together or in any number of other various uses including trim for FRP panels, Rigid Plastic wall panels, termination trims for gypsum board, ceramic tile, stone tile, wood panels, rigid sheet vinyl wall covering, etc.

Section may be used alone or product information may be copied and placed within another section such as FRP when used as a trim for FRP, etc.

Stainless Architectural Supply

8661 North 79th Avenue

Peoria, Arizona 85345

(623) 398-7427

www.sasmfg.com

email: sales@sasmfg.com (sales department)

This section is not necessarily all-inclusive as-is or complete for a specific project without careful editing by a technically knowledgeable person familiar with project needs and products and procedures required to properly produce intended results.

It is intended that Specifications be edited to exactly express project work, which requires inapplicable portions of the Section be deleted, and other pertinent project-specific portions added.

Red colored text shown within boxes is included for instructional use for the specifications writer and should be deleted in the final version of the Specification.

Blue text within [brackets] identifies a selection to be made. Select or revise list as required and delete the brackets in the final version of the Specification.

LEED Requirements:  Sample specification language specifying LEED requirements is shown in Green colored text within [brackets]. Delete all LEED requirements if Project is not LEED Certified.

Refer to manufacturer’s literature for technical Information for LEED MR Credits 4.1 and 4.2 for recycled content and IEQ Credit 4.1 for low-emitting materials (installation adhesive).

PART 1		GENERAL

1.01	RELATED DOCUMENTS

A.	Drawings and general provisions of the Contract, including General Conditions and Division 1 Specification Sections apply to this Section.

1.02	SUMMARY

Edit the following list as required.

A.	This Section includes stainless steel sheet wall covering, trim, and installation accessories of the following type:

[1.	Stainless steel sheet wall covering and associated trim.]

[2.	Formed stainless steel trim molding.]

[3.	Formed stainless steel Z-trim molding.]

Edit the following as required for the project. Possible related sections include, but are not limited to the following. Remove sections for products not included in the project and add sections for other related products where trim is installed to rim the material.

B.	Related Sections:

1.	Section 05 58 13 – Stainless Steel Column Covers

2.	Section 06 64 00 – Plastic Paneling

FRP is sometimes specified in Division 09

3.	Section 06 83 16 – Fiberglass Reinforced Paneling (FRP)

4.	Section 09 62 63 – Stainless Steel Wall Base

3.	Section 09 72 16.16 – Rigid-Sheet Vinyl Wall Covering

4.	Section 10 26 13 – Stainless Steel Corner Guards

1.03	SUBMITTALS

Delete submittals not required for Project.

A.	Product Data:  Submit manufacturer's product data for each type of stainless steel [sheet] [and] [trim] specified, including the following:

1.	Installation accessories.

2.	Installation instructions.

Delete the following if not necessary.

B.	Shop Drawings:  Submit shop drawings showing mounting details.

Delete reference to mock-ups if not required. Mock-ups are not typically required for stainless steel sheet wall covering or formed stainless steel trim moldings but may be included as part of larger mock-up assembly showing full wall construction. Edit as required.

C.	Samples:  Submit samples to the Architect for review prior to [constructing job-site mock-ups,] delivering materials to the site or commencing the work in this Section.

Edit number of samples required to suit Project Requirements. Edit to include wall end caps if necessary.

1.	Stainless Steel Sheet Wall Covering: Submit [3]  [ __ ] samples of stainless steel sheet, minimum 8 inches x 8 inches, of each type of stainless steel sheet wall covering required with specified finish.

2.	Formed Stainless Steel Trim Moldings: Submit [3]  [ __ ] samples of formed stainless steel trim molding, minimum 8 inches long of full size trim, of each type of formed stainless steel trim molding required with specified finish.

Delete the following if Project is NOT to be LEED certified. Coordinate requirements with Projects LEED requirements and Scorecard.

[D.	LEED Submittals:

1.	Credit MR 4.1 and Credit MR 4.2 – Recycled Content: Product data and certification letter indicating percentages by weight of post-consumer and pre-consumer recycled content for products having recycled content. Include statement indicating costs for each product having recycled content.

a.	Submit certification of steel process used in the manufacturing of steel items as well as the industry average recycled content per the steel recycling institute.

2.	Credit EQ 4.1 – Adhesives and Sealants:  Submit documentation including statement of VOC content.

1.04	QUALITY ASSURANCE

A.	Installer Qualifications: Installation of work of this Section shall be by a subcontractor approved by the manufacturer with a minimum of 5 years experience in similar work or other decorative metal installations, or similar rigid sheet wall covering and trim materials, having successful in-service performance.

1.05	DELIVERY, STORAGE AND HANDLING

A.	Packing and Shipping:  Deliver materials to site in manufacturer's original unopened packaging with labels intact.  Protect finished surfaces with removable wrapping or protective plastic film which will not bond when exposed to sunlight.

B.	Storage:  Store [stainless steel sheet wall covering] [and] [trim] in manufacturer’s original packaging, off ground, on flat surface, and under cover away from direct sunlight, protected from weather, extreme temperature, moisture or other damage.

C.	Handling:  Handle materials so that surfaces are protected.  Prevent distortion or damage to fabricated pieces.

1.06	PROJECT/SITE CONDITIONS

Edit the following as necessary if base is installed in exterior application.

A.	Environmental Requirements:  Areas to receive [stainless steel sheet wall covering] [and] [trim] shall be enclosed with HVAC in operation and maintaining temperatures within range expected during building occupancy to avoid thermal dimensional change of material after installation.

1.07	SCHEDULING AND SEQUENCING

Edit or delete the following as appropriate for Project Requirements. Add and/or removed finishes as necessary.

A.	Coordination:  Coordinate installation of [stainless steel sheet wall covering] [and] [trim moldings] with associated [stainless steel wall base] [ceramic tile wall finishes] [FRP] [plastic paneling] [ ________ ] and other adjacent floor and wall finishes.

1.08	MAINTENANCE

Delete the following if “attic stock” maintenance materials are not required for the Project. Edit amounts / quantities as required.

A.	Extra Materials:

1.	Furnish [2] lengths of each type of stainless steel trim molding specified, not less than [8’-0”] each, for Owners maintenance use.

PART 2		PRODUCTS

2.01	MANUFACTURERS

A.	Approved Manufacturer: Stainless Architectural Supply www.sasmfg.com

8661 North 79th Avenue

Peoria, Arizona 85345

(623) 398-7427.

email: sales@sasmfg.com (sales department)

2.02	MATERIALS

Type 430 or 304 stainless steel is manufacturer’s standard material. Type 316 may be available. Consult manufacturer for availability.

A.	Stainless Steel Sheet: ASTM A240, Type [430] or [304].

Stainless Steel Sheet Wall Covering is available in 16, 20 and 24 gauge thickness. Formed Stainless Steel Trim Molding is available in 20, 22, or 24 gauge thickness. Formed Stainless Steel Z-Trim Molding is available in 16, 18, 20, 22, or 24 gauge thickness.

Coordinate with model number selected.

Consult manufacturer for availability of other gauges and edit if other gauge is selected.

If multiple gauges are required, remove gauge from below and add the gauge to each product in each of the following product descriptions.

1.	Gauge:  [16] [18] [20] [22] [24] gauge.

No. 4 Brushed finish is standard. 2B mill finish, No.8 mirror finish, and BA bright annealed finish (similar to No. 8) is also available. Consult manufacturer for availability of these finishes and other custom finishes, and edit if another finish is selected.

2.	Finish:  [No. 4 Brushed] [2B mill] [No. 8 mirror] [BA bright annealed] in accordance with ASTM A480.

Retain the following when specifying stainless steel sheet wall covering material. Select size or leave as manufacturer’s responsibility.

3.	Stainless Steel Sheet Size:  [4’ x 8’] [4’ x 10’] [manufacturer’s maximum size to suit project requirements].

Delete the following if Project is NOT to be LEED certified. Coordinate percentage with Projects LEED requirements and Scorecard.

[B.	Recycled Content:  Stainless steel shall have a postconsumer recycled content plus one-half of preconsumer recycled content of not less than 25 percent.]

2.03	FORMED STAINLESS STEEL TRIM MOLDING

Select type(s) of formed stainless steel trim moldings desired for Project in either Type 430 or Type 304 stainless steel. Consult manufacturer’s current product catalog and edit as necessary.

Select the following for Type 430 stainless steel trim molding.

[A.	Type 430 Stainless Steel Trim Molding:]

Consult manufacturer’s catalog for formed trim molding model number and make selections from model number below. Model numbers below are for 24 ga. with No. 4 brushed finish in either 8 foot or 10 foot length. Edit as required for other finishes.

[1.	CAP: Model [CA-1 08] [CA-1 10]

[2.	DIVIDER: Model [D-1 08] [D-1 10]

[3.	INSIDE CORNER: Model [IC-1 08] [IC-1 10]

[4.	OUTSIDE CORNER: Model [OC-1 08] [OC-1 10]

Select the following for Type 304 stainless steel trim molding.

[A.	Type 304 Stainless Steel Trim Molding:]

Consult manufacturer’s catalog for formed trim molding model number and make selections from model number below. Model numbers below are for 24 ga. with No. 4 brushed finish in either 8 foot or 10 foot length. Edit as required for other finishes.

[1.	CAP: Model [CA-11 08] [CA-11 10]

[2.	DIVIDER: Model [D-11 08] [D-11 10]

[3.	INSIDE CORNER: Model [IC-11 08] [IC-11 10]

[4.	OUTSIDE CORNER: Model [OC-11 08] [OC-11 10]

2.04	FORMED STAINLESS STEEL Z-TRIM MOLDING

Select type(s) of formed stainless steel Z-trim moldings desired for Project in either Type 430 or Type 304 stainless steel. Consult manufacturer’s current product catalog and edit as necessary.

Select the following for Type 430 stainless steel Z-trim molding.

[A.	Type 430 Stainless Steel Z-Trim Molding:]

Consult manufacturer’s catalog for formed Z-trim molding model number and make selections from model number below. Model numbers below are for gauge indicated with No. 4 brushed finish in either 8 foot or 10 foot length. Edit as required for other finishes.

[1.	ZTRIM: Model [ZT-108] [ZT-110], 24 gauge

[2.	ZTRIM: Model [ZT-208] [ZT-210], 22 gauge

[3.	ZTRIM: Model [ZT-308] [ZT-310], 20 gauge

[4.	ZTRIM: Model [ZT-408] [ZT-410], 18 gauge

[5.	ZTRIM: Model [ZT-508] [ZT-510], 16 gauge

Select the following if pre-drilled holes are desired for installation.

[6.	Pre-Drilled: Provide Z-trim with pre-drilled holes located at 16 inches center to center.]

Select the following for Type 304 stainless steel Z-trim molding.

[A.	Type 304 Stainless Steel Z-Trim Molding:]

Consult manufacturer’s catalog for formed Z-trim molding model number and make selections from model number below. Model numbers below are for gauge indicated with No. 4 brushed finish in either 8 foot or 10 foot length. Edit as required for other finishes.

[1.	ZTRIM: Model [ZT-1108] [ZT-1110], 24 gauge

[2.	ZTRIM: Model [ZT-2208] [ZT-2210], 22 gauge

[3.	ZTRIM: Model [ZT-3308] [ZT-3310], 20 gauge

[4.	ZTRIM: Model [ZT-4408] [ZT-4410], 18 gauge

[5.	ZTRIM: Model [ZT-5508] [ZT-5510], 16 gauge

Select the following if pre-drilled holes are desired for installation.

[6.	Pre-Drilled: Provide Z-trim with pre-drilled holes located at 16 inches center to center.]

2.06	INSTALLATION ACCESSORIES

Delete the following if Project is NOT to be LEED certified. Coordinate requirements with Projects LEED requirements and Scorecard. Adhesive products also comply with Greenseal GS-26, SCAQMD, CARB and NAHB Green Building Specifications.

[A.	LEED Requirements:  Adhesive shall have a VOC content of 50 g/L or less when calculated according to 40CFR 59, Subpart D (EPA Method 24).]

Select type of adhesive desired for Project.

Polymer Adhesive Coverage Rate: 160 sq. ft. using V-notch 3/16 inch x 1/4 inch x 5/16 inch trowel.

[B.	Adhesive: Manufacturer’s standard VOC compliant polymer adhesive supplied in 3.5 gallon bucket.]

[B.	Adhesive: Manufacturer’s standard polyurethane adhesive supplied in 10.5 oz or 29.0 oz tubes.]

[B.	Adhesive: Pecora 895 NST Adhesive.]

Delete below if fasteners are not used for installation. Adhesive installation is standard method of installation in most cases. Fastener installation is available when units are specified with optional holes. Edit the following if another head type is desired.

[C.	Fasteners: #10 stainless steel screws with flat pan head to be set flush.]

2.07	FABRICATION

A.	Formed stainless steel trim moldings shall be factory formed from stainless steel sheet with directional polish grain oriented parallel with length.

1.	Edges shall be free of burrs.

Delete the following if Z-trim is installed with adhesive only.

2.	Fabricate Z-trim with pre-drilled and countersink holes spaced at 16 inches center to center for seating of flush fasteners where trim is indicated to be installed with fasteners.

PART 3		EXECUTION

3.01	EXAMINATION

A.	Verification of Conditions:  Examine subsurfaces to receive Work and report detrimental conditions in writing to Architect.  Commencement of Work will be construed as acceptance of subsurfaces.

Revise the following two paragraphs as necessary for type of walls where stainless steel sheet wall covering and/or formed stainless steel trim will be installed.

1.	Painted walls shall be dry and thoroughly cured prior to application of stainless steel sheet wall covering and trim.

2.	Perform adhesion test on painted drywall or plaster walls to receive stainless steel sheet wall covering in accordance with manufacturer’s installation instructions to verify proper adhesion.

B.	Coordination:  Coordinate with other work which affects, connects with, or will be concealed by this Work.

1.	Coordinate installation of formed stainless steel trim moldings with application of wall finishes.

2.	Verify application of wall finish is completed and ready for installation of trim.

3.02	PREPARATION

A.	Surface Preparation:  Surfaces to receive stainless steel sheet wall covering and trim shall be cleaned to remove all dust, debris, and other contaminates that would interfere with adhesive bond.

B.	Place stainless steel sheet wall covering and trim in locations/rooms where units will be installed and acclimate to building conditions as specified herein in Project/Site Conditions article for a minimum period of 24 hours prior to installation.

3.03	INSTALLATION

Adhesive installation is preferred method of installation for most cases.

A.	Adhesive Installation: Install stainless steel sheet wall covering and trim with adhesive in strict accordance with manufacturer’s printed installation instructions.

Edit the following if another head type is desired.

[A.	Fastener Installation: Install formed stainless steel Z-trim with countersunk #10 stainless steel screws placed in pre-drilled and countersunk holes. Tighten screw heads flush in countersunk hole.

3.04	Damage and Repair

A.	Upon completion of the installation, visually check exposed surfaces of the work of this Section, and touch up scratches and damaged surfaces by field polishing so they are completely invisible to the unaided eye from a distance of five feet.

3.05	Cleaning

A.	Upon completion of installation of stainless steel sheet wall covering and trim, promptly clean exposed surfaces in accordance with recommendations of the stainless steel sheet wall covering and trim manufacturer to remove all traces of dust, dirt, adhesive, and other foreign materials.

B.	During the course of the Work and on completion, remove and dispose of excess materials, equipment and debris away from premises.  Leave Work in clean condition.

END OF SECTION